CHAPTER THREE

EXPERIMENTAL WORK

3.1 Elements of  Experimental Work

3.1.1 CNC turning machine

All machining experiments were carried out in Arabian Golf Oil company on a Mori Seiki SL-15 CNC Latheas shown in Fig. 3.1, with specifications that summarized in Table 3.1 .Various combinations of cuttingspeed , feed and depth of cut were chosen for the tests with the aim of providing additional tool wear data; this was to ensure the proper construction of tool life model.

Fig.3.1 Mori Seiki SL-15 CNC Lathe

Table3.1.1 Mori Seiki SL-15 CNC Lathe Specifications

| Maximum Turn Diameter | 9.06" | 230 mm |
| --- | --- | --- |
| Distance between centers | 24.8" | 630 mm |
| Maximum Turn Length | 20.7" | 526 mm |
| X-Axis travel | 9.1" | 231 mm |
| Z-Axis travel | 20.7" | 526 mm |
| Rapid Traverse | 590 IPM |  |
| Chuck size | 6.0” | 152 mm |
| Hole through spindle | 2.2" | 56 mm |
| Bar capacity: | 1.77" | 50 mm |
| Spindle speeds | 50 - 2000 RPM |  |
| Spindle drive motor | 10 / 15 HP Cont. / 30 min. |  |
| Tool turret | 12 Positions |  |
| Tailstock Quill Travel | 3.15” | 80 mm |
| Floor Space Required | 130” x 51” x 65” | 3302 mm x 1295 mm x 1651 |
| Weight | 6600 lbs. | 2993.71 kg |

Mori Seiki SL-15 CNC lathe has been provided with a spindle load meter , this load meter aids the machinist with a visual display of how hard the spindle motor and drive areworking relative to the limits of the drive system. The spindle load meter can be used to monitor tool wear, as an increase in load over time can be a sign of tool wearand indicate that it is time to re-sharpen or change tools, and can also be usedto modify programs to improve material removal rates while limiting the risk of tool breakage.

3.1.2  Workpiece material

A low alloy steel ( DIN  42CrMo4 ), with hardness, length and diameter of  180 HB,174 mm,78  mm respectively, has been used as a work material.

The turned length is 131 mm,  and the chemical composition is given in Table3.2

Fig.3.2 Work piece material

Table 3. 2 Chemical Composition of Work piece Material (weight %)

| Carbon (C) % | Silicon (Si) % | Manganese (m n) % | Phosphorus (P) % | Sulphur (S) % | Chrome (Cr) % | Molybdenum ( Mo) % |
| --- | --- | --- | --- | --- | --- | --- |
| 0.38-0.45 | 0.40 | 0.6-0.90 | .035 | 0.035 | 0.90-1.2 | 0.15-0.30 |

3.1.3  Work design

1.select kind of material and dimensions (Initialdiameter78mm,final diameter 38mm, the

long of work piece174mm,turned length 131mm).

2.prepare the specimen with the dimensions.

3. set up the machine and choose the cutting tool type

Fig.3.3. set up the machine program

4.apply the final table with the level of variables (feed, depth of cut, cutting speed)

5.measure the flank wear regarding to the cutting every 5minutes.'

3.1.4  Insert bit material

A titanium based cemented carbide with increased contents ofTiN and the binder-phase which results in improved toughness. Combined with the typical advantages of cermet grades such as good resistance to oxidation notch wear and smearing, CT 525 is an excellent grade for finishing and semi-finishing at moderate cutting speed and low to medium feeds of low alloyed and alloyed steels.

Fig.3.4 Insert bit material

3.1.5 Code key for the insert( CCMT 12 04 04 –UF    525 )

Figure.3.2Shows some information about the insert geometry .

Fig3.5 Insert geometry

3.1.6Tool holder

Tool holder is a tool used to rigidly hold a cutting insert in place during machining. Toolholders are classified so that they can be paired with the correct style of insert. The description of used tool holder are summarized in figure (3.3 ), and figure (3.4 ) shows a photo of the used the insert and tool holder.

Fig 3.6 Tool holder description

Fig 3..7 Tool insert with tool holder

3.1.7Cutting fluid

Ultracut 250HW has been used as a cutting fluid, it has the following specifications :

- Formulated for hard water conditions ( above 250 ppm  ).

- Low foaming, it is designed for light to medium cutting operations on ferrous and non-ferrous metals.

- Contains a high percentage of refined mineral oils affording high degree of residual corrosion protection and lubricity whilst machining.

- Rejects tramp oil and forms a milky emulsion when mixed with water.

- Dilution between 15:1 and 35:1

3.1.8Wear criterion

All of the experiments were started with a new cutting edge. Depending on the cutting conditions and wear rate, machining was stopped at various intervals of time to record the wear of the insert. Flank wear has been considered as the criteria for tool failure and the wear was measured by a micrometer,the insert rejected when an average flank wear reaches 0.5 mm was recorded. [12]

3.1.9 Identification and limits of the process variables

The following independently controllable process parameters were identified to carry out the experiments: rotational speed (N), feed (F) and depth of cut (D). , Trial runs were carried out to decide which type of insert used . The working range was decided based on some preliminary tests, and with the advice of head of turning workshop.

: the original value of the parameter

Table3.3Process Control Parameters and Their Levels

| Parameter | Notation | Units | Levels |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  |  | 1 | 2 | 3 |
| A speed | N | m/rev | 120 | 220 | 320 |
| BFeed | F | Mm/rev | 0.3 | 0.6 | 0.9 |
| CDepth of cut | D | mm | 0.7 | 1.4 | 2.1 |

3.2  Experiments Design

Use of Orthogonal Array implies that we cannot or ought not study interactions between control factors. We include only control factors that do not interact with each other, say A, B, C and D.

This is shown inTable 3.4 (use L9 array)

Table 3.4 L9 Array

(3.1)

( 3.2)

(  3.3)

Once these SN ratio values are calculated for each factor and level, they are tabulated as shown below and the range R (R = high SN - low SN)of the SN for each parameter is calculated and entered into the table. The larger the R value for a parameter, the larger the effect the variable has on the process. This is because the same change in signal causes a larger effect on the output variable being measured.

Table 3.5 Relationship BetweenRank of Level

3.3 Effect Parameters of  Tool Life Model Using the Taguchi Approach and Response Surface Methodology

The objective of this research is to compare the cutting parameters of turningoperation the work pieces ofby finding low alloy steel ( DIN  42CrMo4 ),)  the longest

tool life by Taguchi methods and Response SurfaceMethodology: RSM. This research is to test the collectingdata by Taguchi method. The analyses of the impact

Table 3.6 parameters of Tool Life Model.

| Std | Run | Factor 1 A:Speed m/min | Factor 2 B:Feed mm | Factor 3 C:Depth mm | Response 1 Tool l min |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | RUN1 | RUN2 | RUN3 | AVREG |
| 8 | 1 | 320 | 0.6 | 0.7 | 4.48 | 5.25 | 5.31 | 5.01 |
| 6 | 2 | 220 | 0.9 | 0.7 | 20 | 18.5 | 21 | 19.5 |
| 9 | 3 | 320 | 0.9 | 1.4 | 5.1 | 4 | 4.5 | 4.5 |
| 5 | 4 | 220 | 0.6 | 2.1 | 16.6 | 15.9 | 17 | 16.5 |
| 1 | 5 | 120 | 0.3 | 0.7 | 30 | 28.4 | 29 | 29.13 |
| 2 | 6 | 120 | 0.6 | 1.4 | 29 | 28.5 | 27 | 28.16 |
| 3 | 7 | 120 | 0.9 | 2.1 | 28.3 | 27.2 | 29 | 28.1 |
| 7 | 8 | 320 | 0.3 | 2.1 | 5.1 | 4.5 | 4 | 4.53 |
| 4 | 9 | 220 | 0.3 | 1.4 | 19.9 | 20 | 20.3 | 20.0 |

Fig.3.5A detailed Description of The execution of These steps Will be Discussed next.